Properties of Debonder

| Debonder | Nitromethane | DMF | Acetone | Dimethyl Sulphoxide |
| --- | --- | --- | --- | --- |
| Properties |  |  |  |  |
| Chemical Formula | CH3 NO2 | HCON(CH3)2 | (CH3)2 CO | (CH3)2 SO |
| Appearance | Colorless Liquid | Colorless Liquid | Colorless Liquid | Colorless Liquid |
| Odor | None | Amine-like Odor | Peppermint Odor | None |
| Boiling Point | 214.2˚F | 301.3˚F | 133.2˚F | 372.2˚F |
| Flash Point | 111.2˚F | 154.4˚F | 1.4˚F | 203˚F |
| Ignition Point | 784.4˚F | 1072.4˚F | 1202˚F | - |
| Solubility in Water | Hardly Soluble | Soluble | Soluble | Soluble |
| Tolerance | 100 PPM | 10 PPM | 1,000 PPM | - |
| Notes | - | Toxic Cautious handling is necessary | Volatile Extremely flamable | Does not corrode styrene and methyl methacrylate |

*Polymer of Methyl 2-cyanoacrylate such as Type 101 is insoluble in Acetone.  Use Nitromethane, DMF, or Dimethyl Sulphoxide to dissolve Methyl 2-cyanoacrylate polymer.

Solubility of Plastics in Debonder and Surface Activator

|  | Debonder |  |  |  | Surface Activator |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Chemicals | Nitromethane | DMF | Acetone | Dimethyl- Sulphoxide | Methyl Chloroform | 5% NaOH Solution | Accelerator* |
| Adherend |  |  |  |  |  |  |  |
| Rigid PVC | O | X | O | O | O | O | O |
| Soft PVC | O | X | O | O | O | O | O |
| PMMA | X | X | X | O |  | O | X |
| Polycarbonate | O | X | X | X | X | O | X |
| Polystyrene | O | X | X | O | X | O | X |
| Nylon | O | O | O | O | O | O | O |
| Polyester | O | O | O | O | O | O | O |
| ABS | X | X | X | X | X | O | X |
| AS | X | X | X | X | X | O | X |
| Polyacetal | O | O | O | O | O | O | O |
| Acetal Copolymer | O | O | O | O | O | O | O |
| Urea Resin | O | O | O | O | O | O | O |
| Phenolic | O | O | O | O | O | O | O |
| Melamine | O | O | O | O | O | O | O |
| Celluloid | X | X | X | X | O | O | X |
| Acetyl Cellulose | X | X | X | O | X | O | X |
| Natural Rubber | O | O | O | O | O | O | O |
| Neoprene Rubber | O | O | O | O | O | O | O |

Note:  10 minute immersion at room temperature.  					*Acetone Based

O: No Change		: Surface slightly eroded	X: Surface becomes sticky