Chemical Resistance (Immersion Time vs. Strength)

The bonded and cured specimens are immersed in the chemicals.  The specimens are taken out of the bath after a certain interval of time and the tensile strength is determined.

|  | Adherend | Tensile Strength (psi) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Before Immersion | After 3 months | After 6 months | After 1 year | After 3 years |
| Gasoline | Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 |
|  | ABS | *3560 | *3560 | *3560 | *3560 | *3560 |
|  | Phenolic | *4980 | *4980 | *4980 | *4980 | *4980 |
|  | Neoprene Rubber | *360 | *360# | *360# | *360# | *140# |
|  | Steel | 4550 | 4550 | 4550 | 4550 | 4550 |
|  | Copper | 4980 | 4980 | 4980 | 4980 | 4980 |
| Kerosene | Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 |
|  | ABS | *3560 | *3560 | *3560 | *3560 | *3560 |
|  | Phenolic | *4980 | *4980 | *4980 | *4980 | *4980 |
|  | Neoprene Rubber | *360 | *360# | *360# | *360# | *360# |
|  | Steel | 4550 | 4550 | 4550 | 4550 | 4550 |
|  | Copper | 4980 | 4980 | 4980 | 4980 | 4980 |
| Mobile Oil | Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 |
|  | ABS | *3560 | *3560 | *3560 | *3560 | *3560 |
|  | Phenolic | *4980 | *4980 | *4980 | *4980 | *4980 |
|  | Neoprene Rubber | *360 | *360# | *360# | *360# | *360# |
|  | Steel | 4550 | 4550 | 4550 | 4550 | 4550 |
|  | Copper | 4980 | 4980 | 4980 | 4980 | 4980 |
| **Freon 11(-4˚F) | Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 |
|  | ABS | *3560 | *3560 | *3560 | *3560 | *3560 |
|  | Phenolic | *4980 | *4980 | *4980 | *4980 | *4980 |
|  | Neoprene Rubber | *360 | *360# | *360# | *280# | *140# |
|  | Steel | 4550 | 4550 | 4550 | 4550 | 4550 |
|  | Copper | 4980 | 4980 | 4980 | 4980 | 4980 |
| 10% Sulfuric Acid | Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 |
|  | ABS | *3560 | *3560 | *3560 | *3560 | *3560 |
|  | Phenolic | *4980 | 2130 | 0 | - | - |
|  | Neoprene Rubber | . | *360 | *360 | *360 | *360 |
|  | Steel | 4550 | 0 | - | - | - |
|  | Copper | 4980 | 4980 | 4980 | 4980 | 4980 |

* Material Failure

** DuPont Trademark

# Material Deformed

Test Conditions

- Test specimen……………..  0.5 x 0.5 x 1.5 in

- Surface treatment…………  Polished with smooth-cut file and degreased with methyl chloroform

- Bonding atmosphere………  73.5˚F, 60% RH

- Speed of load………………  20 mm (0.8in) /min.

- Water………………………  Stored at room temperature

- Adhesive…………………..  Aron Alpha Type 201

- Test Method………………..  ASTM D 2095