Weather Resistance

1. Outdoor Exposure Test

|  | Before Exposure | 6 months | 1 year | 2 years | 3 years | 5 years |
| --- | --- | --- | --- | --- | --- | --- |
| Adherend | psi | psi | psi | psi | psi | psi |
| Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 | 4980 |
| ABS | *3560 | *3560 | *3560 | *3560 | *3560 | *2840 |
| Phenolic | *4980 | 710 | 0 | - | - | - |
| Neoprene Rubber | *360 | *360 | *360 | *360 | *360 | *280 |
| Steel | 4550 | 0 | - | - | - | - |
| Copper | 4980 | 4980 | 4980 | 4980 | 4980 | 4980 |

*Material Failure

2.  Indoor Durability Test

|  | Tensile Strength |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Before Exposure | 6 months | 1 year | 2 years | 3 years | 5 years |
| Adherend | psi | psi | psi | psi | psi | psi |
| Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 | 4980 |
| ABS | *3560 | *3560 | *3560 | *3560 | *3560 | *3560 |
| Phenolic | *4980 | *4980 | *4980 | *4980 | *4980 | *4980 |
| Neoprene Rubber | *360 | *360 | *360 | *360 | *360 | *360 |
| Steel | 4550 | 4550 | 4550 | 4550 | 4550 | 4550 |
| Copper | 4980 | 4980 | 4980 | 4980 | 4980 | 4980 |

*Material Failure

3.  Accelerated Weathering Test by Weather-meter

|  | Before Exposure | 6 months | 1 year | 2 years | 3 years | 5 years |
| --- | --- | --- | --- | --- | --- | --- |
| Adherend | psi | psi | psi | psi | psi | psi |
| Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 | 4980 |
| ABS | *3560 | *3560 | *3560 | *3560 | *3560 | *3560 |
| Neoprene Rubber | *360 | *360 | *360 | *360 | *360 | *360 |
| Steel | 4550 | 4270 | 3840 | 2560 | 1850 | 1420 |
| Copper | 4980 | 4980 | 4980 | 4980 | 4980 | 4980 |

*Material Failure

Test Conditions

- Test specimen……………..  0.5 x 0.5 x 1.5 in

- Surface treatment…………  Polished with smooth-cut file and degreased with methyl chloroform

- Bonding atmosphere………  73.5˚F, 60% RH

- Curing Time………………..  24 hours under above atmosphere

- Speed of load………………  20 mm (0.8 in)/min

- Adhesive…………………...  Aron Alpha Type 201

- Test Method………………..  ASTM D 2095